Mauveine and the mauve shade six pence stamp

M. John Plater* and Andrea Raab

Department of Chemistry, University of Aberdeen, Meston Walk, Aberdeen AB24 3UE,UK

Key words: William Henry Perkin, mauveine, mauve, victorian stamps, six pence

Table of contents

M. J. Plater and A. Raab

Abstract

Victorian six pence lilac stamps, plate 5, 6, 8, and 9 have been analysed for mauveine: six pence stamps, no hyphen and plate 8 or 9, were dyed with mauveine, six-pence stamps with the hyphen, plate 5, were not dyed with mauveine, about half of the six-pence stamps with the hyphen, plate 6, were dyed with mauveine, and one six-pence stamp with the hypen, plate 6, analysed as being dyed with Caro’s mauveine.

Introduction

Memorabilia of mauveine includes various bottles of mauveine housed in museums in London (Science Museum),1 Manchester (Museum of Science and Industry),2 Bradford (Colour Experience Museum),3 New York (Columbia University)4 and Germany (Deutsche Museum).5 There are also mauveine dyed dresses1,6 and silks,1 letters,2,7  stamps, photographs8 and a silver tea set.3 The silver tea set was given to WH Perkin in 1906 to mark the occasion of the Jubilee celebration of the discovery of mauve in 1856 (Figure 1). It is embossed with a structure for pseudo-mauveine, a coumarin synthesis and some of WH Perkins achievements in alizarin synthesis. The structure for pseudo-mauveine has the 2 and 3 methyl groups of mauveine A and B respectively, removed. The X-ray single crystal structure of pseudo-mauveine was recently determined which confirmed the structure and positions of the hydrogens on the nitrogens.9

Figure 1 The Colour Experience Museum display cabinet on mauveine showing a dress, silks, bottles of mauveine, original photographs of WH Perkin and the golden jubilee 1906 tea set.

The victorian 1881 one penny postage stamp has often been considered as a mauveine dyed stamp but recently this was shown to be incorrect.10 Our study here analyses stamps making use of the Stanley Gibbons (SG) Great Britain specialised stamp catalogue.11 This is a detailed and accurate record of the stamps which were published in this period. The catalogue lists stamps by shade and is supplemented by an SG shade card which has some shades of mauve such as deep mauve and bright mauve. Mauve refers to a shade but not necessarily to mauveine dye. The chemical names of dyes were not used in the catalogue.

Discussion

Mauve analysis in stamps by LC-MS

Mauveine was analysed for in 15 used six pence lilac stamps by extraction with MeOH and then analysis by LC-MS. Figure 2 shows the LC-MS analysis of archived mauveine from the Manchester Museum of Science and Industry, figure 3 shows the LC-MS analysis of mauveine synthesised by a method similar to that of WH Perkin’s patent,12, figure 4 shows the LC-MS analysis of some lilac 1865-1869 victorian six pence stamps and a six pence stamp coloured with Caro’s mauveine. Tables 1-6 in the supplementary section give information on relative peak integrations and table 7 in the text gives some information on the molecular structures. The other stamp chromatograms and analyses of the compositions are given in the supplementary section. The first two analyses are control experiments for comparison with mauveine from the stamps. A comparison of archived mauveine and mauveine synthesised by WH Perkin’s method has been made elsewhere.13-17 Mauveine from six pence stamps is rich in mauveine A with a lesser amount of mauveine B as reported before.10 The common 1881 penny lilac, 30 stamps, were not dyed with mauveine in agreement with literature results.10

Figure 2 LC-MS analysis of archived mauveine from the Manchester Museum of Science and Industry.

Figure 3 LC-MS analysis of mauveine made by a method similar to WH Perkin’s patented method and is described in the experimental section.

(a)

(b)

(c)

Figure 4  LC-MS analysis of the mauveine extracted from lilac Victorian six pence stamps with MeOH. Top: (a) six pence plate 8 or 9; Middle : (b) six-pence plate 6; (c) Bottom: six-pence plate 6 which is Caro’s mauveine. For figures 4(d-h)  and  tables (1-6) of peak integrations see  supplementary section.

| m/z | Number of carbons | Name |
| --- | --- | --- |
| 363 | C24 | Pseudo-mauveine |
| 377 | C25 | Mauveine C25a, C25b, C25c |
| 391 | C26 | Mauveine A, A1 |
| 405 | C27 | Mauveine B, B2, B3, B4 |
| 419 | C28 | Mauveine C, C1 |
| 433 | C29 | Mauveine D |

Table 7 Summary of the mauveine structures seen in the LC-MS charts.

Mauve six pence stamps

Figure 5 shows a stamp from the Stanley Gibbons GB specialised stamp catalogue and three used stamps which analysed as being dyed with mauveine. This stamp is listed as a mauve stamp and was analysed previously.10 However, noteworthy is the catalogue entry that it must have no hyphen between the six and pence and it is plate 8 or 9 only.   The plate is the number in the lower right and left corners.  Two shown are plate 8 and the other is plate 9.    Plate 9 six pence stamps are only catalogued as mauve but plate 8 six pence stamps are catalogued as dull violet or mauve. In this study only mauveine-containing stamps were found.  Figure 4a shows a typical LC-MS chart.   The mauveine chromophores are typically in the range  391-419 with a smaller amout of 377 present.

Figure 5 Left: Entry of the mauve six pence stamp in the Stanley Gibbons GB specialised stamp catalogue, no hyphen between six and pence. Catalogue details: SG 108-109 1869 (8 March). 6d. Mauve, Type J15. Wmk Spray (W7). Perf 14.; Right: Three used mauve 6d stamps, catalogue entry on the left,  no hyphen between six and pence. These stamps are plate 8 or 9 and all analysed as being dyed with mauveine. Plate 10 was not published.

Figure 6 shows a lilac stamp from the Stanley Gibbons GB specialised stamp catalogue and a used stamp with the same plate number 6. This stamp is similar to that shown in figure 5 except that it has a hypen between the six and pence and a lower plate number of 6 which is not calalogued as mauve. The SG catalogue also has the same stamp with a plate number of 5. None of the stamps with a plate number of 5 analysed as containing mauveine but about half of those with a plate number of 6 did analyse as containing mauveine. With a trained eye the mauveine-containing plate 6 stamps can be spotted because they have a deeper purple shade than the others.

Figure 6  Left: Entry of a lilac six pence stamp in the Stanley Gibbons GB specialised stamp catalogue, a hyphen between six and pence. Catalogue details: SG 104-107 1867 (21 June). 6d. Lilac, Type J14. Wmk Spray (W7) (plate 6).  Perf 14 or SG 96-97 1865 (7 March). 6d., Type J14. Wmk Emblems (W6). Perf 14 (plate 5) Right : Plate 6 lilac used stamp, catalogue entry on the left, with a hyphen between the six and pence.

Figure 4b shows the predominance of mauveine A in this stamp. The mauveine chromophores still range from 363-419 and are complex. Different stamps illustrate the slight variations in the synthesis conditions probably due to impure aniline or variations in the ratio’s of components. These approximate compositions can be repeated using the novel method suggested for making museum archived mauveine,9,15 but following WH Perkin’s patented procedure and variations of it we did not succeed in preparing mauveine dominated by mauveine A with mauveine B such a minor component. Mauveine A was still formed along with mauveines B, B2 and C with lower amounts of toluidines in the mix.

Recently a report appeared of a six pence lilac stamp plate 6 which analysed as being dyed with Caro’s mauveine10 (SG 104-107). This is most unusual, but pleasingly with some persistence, after analysing about 8 plate 6 stamps, one was found (Figure 4c). The mauveine is dominated by pseudo-mauveine and a monomethyl chromophore  (C25a, C25b, C25c) with two weaker mauveine A chromophores. This mauveine has a very different composition to WH Perkin’s mauveine and a different method of synthesis seems reasonable. It is however not the same as Schunck’s mauveine18 which has  more pseudo-mauveine. HPLC chart’s were published in  some past papers.10,19 Table 8 shows a summary of the composition of Schunck’s and Caro’s mauveine with that of the two Caro’s mauveine stamps that have been found. The higher percentage of the C25 isomers in the six pence stamp, compared to pseudo-mauveine, is quite distinctive.

| Origin10 | Pseudo-mauveine % | C25 mauveines % |
| --- | --- | --- |
| Schunck’s mauveine | 51.71 | 35.32 |
| Caro’s mauveine | 56.11 | 35.70 |
| 6d stamp | 34.15 | 40.21 |
| 6d stamp (this paper) | 19.20 | 36.10 |

Table 8 Comparison of Schunck’s and Caro’s mauveine with two six pence stamps. For the six pence stamp analysed here peaks at 5.1 min (12.70%) and 5.4 min (11.90 %) are mainly m/z 391.

Conclusion

The results are summarised in  table 9 below. No examples of the 1881 penny lilac stamp were found which contained mauveine. All of the six pence plate 8 and 9 stamps that were analysed contained mauveine. No plate 5 stamps analysed as containing mauveine but about half of the plate 6 stamps did. One example of a plate 6 stamp was found consisting of a mixture of pseudo-mauveine, a monomethyl mauveine chromophore (C25a, C25b, C25c)  and a smaller amount of 2 mauveine A isomers. Mauve plate 6 stamps have a deeper purple tone compared to the non-mauve plate 6 stamps. The SG shade of stamps which contain mauveine is either mauve, purple, bright violet or deep lilac. The results of the study are tabulated below.

| Stamp | Stamp detail | Plate | Observations |
| --- | --- | --- | --- |
| SG 170-174 | Penny lilac | - | No examples were dyed with mauveine |
| SG108-109 | six pence no hyphen | plate 8 or 9 | All examples were dyed with mauveine |
| SG 96-97 | six-pence with hyphen | plate 5 | No examples were dyed with mauveine |
| SG104-107 | six-pence with hyphen | plate 6 | About half the examples were were dyed with mauveine |
| SG104-107 | six-pence with hyphen | Plate 6 | One was dyed with pseudo-mauveine + C25a-c + 2 mauveine A isomers |

Table 9 Summary of mauveine analysis in Victorian six pence stamps

Supplementary: LC-MS conditions, six tables of mauveine peak integrations (Tables 1-6), five LC-MS charts (Figure 4d-h)

Experimental

LC-MS

For analytical separation an Agilent 1290 Infinity HPLC system consisting of a quaternary HPLC-pump, cooled auto sampler compartment, column compartment and diode-array UV/VIS-detector was used. A Gold C-18 column (2.1 x 150 mm, Thermo Scientific, UK) was used for separation with a water/methanol gradient (both 0.1 % v/v formic acid) from 40 % MeOH to 100% in 7 min. The flow rate was 0.5 mL/min, column temperature 40 ºC and sample volume 5 µL. The mass spectrometer (ESMS) used was a MAXIS II UHR-TOF LC-MS System, Bruker UK Ltd with ESI source connected to the UV/VIS-detector via a short length of Peek-tubing. The ESMS was operated in positive ion mode with a capillary voltage of 4.5 kV using Na-formate clusters for calibration and methylstereate as lock-mass. MS2 spectra very recorded automatically, but where due to the nature of the molecules not very informative.

Sinters are cleaned with bleach.

Stamp extraction Each stamp was placed in a small sample vial (2 cm x 3cm) and rolled with some MeOH (2 ml) for 2 min. The MeOH was removed and placed in a sample vial for analysis. The stamp was removed carefully from the vial and held on a flat surface to dry. No acid was used which might degrade the paper.

Preparation of the standard mixture of mauveine A, B2, B and C 12,20-26 WARNING: cNH3/MeOH is always used in a fume hood. The method is simple and effective. Some explanatary notes are added. This is a larger scale preparation but the reagents can be scaled down accordingly. p-Toluidine (1.0 g, 9.3 mmol, 1.0 eq), o-toluidine (1.5 g, 14.0 mmol, 1.5 eq) and aniline (1.3 g, 14.0 mmol, 1.5 eq) in water (200 ml) acidified with cH2SO4 (30 drops from a 15 cm long pipette or estimated as 0. 5 ml) were heated to 50-60 0C and treated with K2Cr2O7 (4.6 g, 15.6 mmol, 1.67 eq). The oxidant is the correct calculated amount of 1 2/3 moles to form mauveine. The mixture was heated in a beaker with stirring for 4 h. It was then allowed to cool, although hot filtration is also possible as the dye binds onto polyaniline by-product, filtered through a fine pore sinter No 4 and washed with plenty of water (300 ml).  The precipitate was not dried further as we found this makes the recovery of mauveine more difficult. The precipitate was extracted repeatedly with MeOH (50 ml) about 10 times in the sinter each time agitating the preciptate with a spatula. The combined MeOH extracts from the Buchner flask were evaporated to dryness and purified by chromatography on flash silica gel. A column of dimensions 2.5 cm x 20 cm was used. The column is loaded by agitating the precipitate with MeOH (80 ml) then pouring on top of the silica and eluting down the head volume. This may be repeated once. The eluent MeOH is used initially to remove brown polyaniline by-product followed by cNH3/MeOH (20: 80) to elute the mauveine. MeOH is highly effective at initially removing brown polyaniline by-product which WH Perkin removed by solvent extraction  and the mauveine sticks quite well on the silica with MeOH as eluent. The mauveine dye elutes in a beautiful purple column. The  fractions were analysed by TLC. The TLC eluent cNH3/MeOH (20:80)  is fastest but does not separate the mauveine chromophores. To analyse the mauveine chromophores sec-butanol/EtOAc/H2O/HOAc (60:30:9.5:0.5) is used.27-28 The combined pure fractions were evaporated in a beaker on a hot plate in a fume hood with the fan on so the ammonia vapour is always kept in the fume hood. A yield of 82 mg (0.184 mmol, 2.0%) was obtained estimating an average molecular weight of 446 (2.5 methyl groups and half a sulfate)

References

1. Science Museum, Exhibition Road, London, SW7 2DD and Blythe House, Blythe Road, West Kensington, W14 0QX.

2. Manchester Museum of Science and Industry, Liverpool Road, Manchester, M3 4FP.

3. The Colour Experience Museum, Society of Dyers and Colourists, Perkin House, 82 Grattan Road, Bradford, West Yorkshire, BD1 2LU, England.

4. Chandler Museum Collection, Department of Chemistry, Columbia University, 344 Havemeyer Hall, MC 3178.

5. Deutsches Museum, Leitung Abteilung Chemie (AI), Museumsinsel 1, 80538 München, Germany.

6. Blakes Museum, 5 Blake St, Bridgwater, TA6 3NB.

7. College Archivist & Corporate Records Manager, Room 455, Sherfield Building, Imperial College, London, SW7 2AZ.

8. Science & Society Picture Library, Science Museum Group Enterprises Ltd, Science Museum Group, Exhibition Road, London, SW7 2DD.

9. M. J. Plater, W. T. A. Harrison and H. S. Rzepa, J. Chem. Res., 2015, 39, 711.

10. M. C. Oliveira, A. Dias, P. Douglas and J. S. S. Melo, Chem. Eur., 2014, 20, 1808.

11. Stanley Gibbons Great Britain specialised stamp catalogue, Vol. 1 Queen Victoria, 9th ed. London, Stanley Gibbons Publications 1989.

12. W.H. Perkin, Patent No 1984, 26th Aug. 1856

13. J. Seixas de Melo, S. Takato, M. Sousa, M. J. Melo and A. J. Parola, Chem.

Commun., 2007, 2624.

14. M. J. Plater, J. Chem. Res., 2014, 38, 163.

15. M. J. Plater and W. T. A. Harrison, J. Chem. Res., 2014, 38, 651.

16. M. J. Plater and A. Raab, J. Chem. Res., 2015, 39, 180.

17. M. J. Plater, J. Chem. Res., 2015, 39, 251.

18. J. Dale and H. Caro, Patent 1860, 26th May, No 1307.

19. M. J. Plater and A. Raab, J. Chem. Res., 2015, 39, 180.

20. M. V. Canamares, D. A. Reagan, J. R. Lombardi and M. Leona, J. Raman Spec., 2014, 45, 1147.

21. M. J. Plater, J. Chem. Res., 2011, 35, 304.

22. T.M. Brown, C.J. Cooksey and A.T. Dronsfield, Educ. Chem., 2000, 37, 75.

23. S. Garfield, Mauve, Faber and Faber, 2000, London.

24. R.L. Scaccia, D. Coughlin and D.W. Ball, J. Chem. Ed., 1998, 75, 769.

25. W.H. Cliffe, J. Soc. Dyers Colourists, 1956, 72, 563.

26. A. Cobenzl, Oesterr. Chem-Ztg., 1925, 28, 25.

27. O. Meth-Cohn and M. Smith, J. Chem. Soc., Perkin Trans., I 1994, 5.

28. O. Meth-Cohn and A.S. Travis, Chem. Brit., 1995, 31, 547.

Acknowledgement

We are grateful to the Manchester Museum of Science and Industry  and to the Bradford Colour Experience Museum.